SPRINT

Specification Sheet

Materials

Pressure Reducing Valve		Anodised Aluminium

Rust Tube				Brass

Reducing Valve Seat			Polyamide (Nylon)

O-Rings				Nitrile, Silicone, EPDM

Reducing Valve Springs		Stainless Steel

HP Pressure Gauge			Stainless Steel, Brass, Polycarbonate Lens

HP Pressure Gauge Cover		Neoprene

MP Air Supply Hose Fittings		Nickel Plated Brass

Air Hood				Polyurethane coated viscose with clear PU visor

Facemask				Neoprene

Facemask visor			Polycarbonate

MP Air Supply Hose			Chlorinated Polyethylene, fabric braid reinforcement, 					nitrile liner

Carrying Bag				PVC Coated Nylon. (Antistatic - Polyurethane)

Valve Handwheel			Glass filled polyamide

Strap Buckles				Polyamide

Cylinder				  5 Min:- Aluminium

10 Min:- Aluminium

15 Min:- Alloy Steel

Cylinder Valve				Anodised Aluminium

Demand Valve Casing		Glass filled polyacetal and polyamide

Weight

5 Minute bag version 			3.5kg

10 Minute bag version 		4.5kg

15 Minute bag version		5.6kg

Dimensions

5 Minute bag version	 		Length:- 29cm Width & Depth:- 21cm

10 Minute bag version 		Length:- 45cm Width & Depth:- 21cm

15 Minute bag version		Length:- 45cm Width & Depth:- 21cm

Packing Specifications

5 Minute version	56x21x18cm		5.5kg

10 Minute version	56x21x18cm 		6.0kg

15 Minute version	56x21x18cm 		6.5kg

Approvals

EN402 	Self rescue self contained open circuit breathing apparatus

Major Components - Sprint

Tempest Demand Valve

Compact positive pressure demand valve featuring servo-assisted, tilting diaphragm mechanism with low inspiratory resistance and responsive dynamic performance.   Automatic first breath actuation is standard although instant positive pressure is available as an option. Components injection moulded from polyamide and acetal with rubber seals and diaphragms.

Peak flow performance:-	in excess of 500 litres/minute

Bypass flow		  :-	150 litres/minute nominal

Static positive pressure:-	1.8 - 3.5 mbar

Pressure reducing Valve

First stage pressure reducing valve featuring non-adjustable, spring loaded piston mechanism and outlet supply protected by an integral pressure relief valve.

Valve body and cap manufactured from lightweight aluminium alloy with anodised protective coating with stainless steel spring and hose retainer U-clips.

Integrated with cylinder valve with a DIN type connection and will accept inlet pressures of up to 300 bar.

Outlet pressure

207 bar inlet:-	5.5 to 9.5 bar

Pressure relief valve protected:- 11.5 bar

Flow restrictor to gauge supply hose <25 litres minute

Cylinder Valve

Manufactured from lightweight aluminium alloy with an anodised protective coating, the valve has a DIN type outlet for connection to the cylinder connector on the PRV and for simple charging. There is a low profile pressure gauge and burst disc assembly incorporated into the Valve and the Handwheel allows for manual or automatic quick-fire activation.

Carrying Bag

The carrying bag is made of PVC coated nylon. This is coloured for high visibility and is both flame retardant and chemical splash resistant. There is an anti-static option for working in potentially explosive atmospheres and this is made of polyurethane.

The bag can be worn across the chest or as a bandolier or there is a waistbelt option.

Demand Flow Hood

This is made from polyurethane coated viscose. This is flame retardant and coloured for high visibility.  This provides a stretch material for a comfortable fit combined with an elastomeric neck seal this gives ease of donning over spectacles, beards and long hair. The optically clear bubble visor is made from polyurethane. The mask has an exhale valve for increased performance and a compact ¼ mask reduces rebreathed CO2 levels.

Hoses

Stainless steel swivel hose fittings

Medium pressure hose

Maximum working pressure	16 bar

Minimum burst pressure	80 bar